The procedure shall be as described in AS 1289.5.4.2 - except where modified or clarified as shown below.

•	Delete references to AS methods and replace with relevant DPTI procedures.

•	Note 3. Where material is not being continuously produced, an update sample for MDD shall be taken at not more than every 1000m3 of production.

•	Forms TP166-1 and TP166-2 may be used for control and charting purposes.

Precision

This procedure is considered to satisfy the accreditation requirements of AS/ISO 17025, Clause 5.4.6 “Estimation of uncertainty of measurement”, sub-clause 5.4.6.2, Note 2.

Department of Planning, Transport & Infrastructure

19 Bridge Rd Walkley Heights (08) 8260 0230, GPO Box 1533, Adelaide 5001

Technical Services Group

# Procedure

# Assigned MDD and OMC Control Data

# TP166

## Material:  		Compaction Procedure AS 1289.5.1.1 & AS 1289.5.2.1	Sheet 	of

| Lot Identification | Individual MDD | Assessment |  |
| --- | --- | --- | --- |
| Sample No. | Lot No. | Project | Date Sampled | Discrete MDD t/m3 | Discrete OMC % | Conforms Y/N | Assn MDD t/m3 | Ass OMC % | Date Assign | Remarks | Calc By |

Form TP166-1, Revn 1.7

Department of Planning, Transport & Infrastructure

19 Bridge Rd Walkley Heights (08) 8260 0230, GPO Box 1533, Adelaide 5001

Technical Services Group

# Procedure

# MDD/OMC Control Chart

# TP166

## Material:  		Sheet 	of  		Charted By

| 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 0 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |

# Form TP166-2, Revn 1.7

# Text boxes

Optimum Moisture Content %

Max Dry Density t/m3